Microstructural Characterization of Carbides in Cryotreated M35High Speed Tool steel by Electron Probe Micro-Analysis Technique

Satish N. Kadu             (Third year B.Tech)

Ishant R. Bhoskar        (Third year B .Tech)

Dept. of Metallurgy and Materials Science

College Of Engineering, Pune-05

(An Autonomous Institute of Govt. of Maharashtra)

Guided By

Dr.Pranesh Sengupta

Materials Science Division

MATERIALS SCIENCE DIVISION

BHABA ATOMIC RESEARCH CENTRE

TROMBAY, MUMBAI- 400 085

AKNOWLEDGEMENT

We take this opportunity to express our deep gratitude to Dr.G.K.Dey, Head, Materials Science Division and Dr. R.R.Puri, Head, Human Resource Division, Bhabha Atomic Research Centre, who have accepted our application for giving us the opportunity to learn here and doing Project Work.

We are very much thankful to Dr. P. Sengupta and Mr. A. Laik, Materials Science Division, BARC, for their invaluable guidance throughout the Project work period without which it would not have been possible to complete the project work in stipulated time. We would also like to thank Mr. Gawde for their support.

We are also very thankful to Dr. Dhokey,College Of Engineering, Pune and Dr. Rathod ,Head ,Department of Metallurgy and Material science, College Of Engineering ,Pune who inspired and guided us to carryout this project work.

CONTENTS

Chapters                                                                                           Page Number

Chapter I: Introduction

1.1 High Speed Tool Steels (HSS)

1.2 Effect of Cryotreatment on microstructure and Properties of M35 HSS

1.3 Objectives and Scope                                                …………………

Chapter II: Experimental Procedure

2.1 Sample Preparation for EPMA

2.2 Characterization Techniques: EPMA and TEM

Chapter III:  Results and Discussion

3.1 Optical and Back Scattered Electron Image of M35 HTC

3.2 Qualitative Analysis of Carbides

3.3 Distribution of Alloying Elements

3.4 X-ray line scan of carbide

3.5 Comparison of Carbide size, shape and Morphology

Chapter IV: Summary

List of Tables, Abbreviations and Symbols

| Table Number | Name | Page Number |
| --- | --- | --- |
| 1.1 | Composition of M35 | 6 |

| Abbreviation | Meaning | Page number |
| --- | --- | --- |
| M35 HTTT | Hardened and triple tempered | 8 |
| M35 HTC16 | Hardened, tempered and Cryotreated at -1860C for 16 Hours | 8 |
| M35 HTC40 | Hardened, tempered and cryotreated at -186oC for 40 hours | 8 |
| M35 HTC48 | Hardened, tempered and Cryotreated at -186oC for 48 hours | 8 |

List of Symbols

| Cr | Chromium |
| --- | --- |
| W | Tungsten |
| Mo | Molybdenum |
| V | Vanadium |
| C | Carbon |

Abstract

The High speed tool steel is an important member of cutting tool materials and is widely used for high speed cutting of materials even at elevated temperatures. In order to eliminate large amount of retained austenite and to increase the Wear resistance, these steels are subjected to cryotreatment.

In the present work, Microstructural characterization of Carbides of M35 Cryotreated high speed tool steel subjected to varying degree of cryosoaking time was done by Electron probe Micro-Analysis. The EPMA analysis using WDS and EDS confirms the presence of W and V rich carbides in the matrix. Some amount of Mo precipitation is also seen. The carbide morphology and carbide density doesn’t found to be changed significantly.

Chapter I

INTRODUCTION

1.1 Tool steels:-

These steels are specially used for working, shaping and cutting of metals. Large numbers of steels are available for this purpose. They are classified and designated according to American Iron and Steel institute (AISI) as below:-

i) Cold work tool steels

ii) Hot Work tool steels

iii) High speed tool steels (HSS)

iv) Special purpose tool steels

Among these, High speed tool steels which is our topic of interest  are used as cutting tools operating at high speeds and elevated temperatures.

1.1.2 High Speed Tool Steels (HSS):

This particular category of tool steels retain their High hardness and Strength even upto a temperature of about 5500C and hence can be used for cutting of metals at high speeds at elevated temperatures.

High Speed Steels are divided into two types depending upon the principle alloying element.

1) Tungsten High Speed Steels:-

These steels contain high amount of tungsten (W), with other elements such as Cr, V And Co. They are designated by T-series. The most widely used grade is T1 grade.

2) Molybdenum High Speed Steels:-

A part of tungsten from the group of tungsten high speed steels is substituted by Molybdenum and hence these steel contains W, Cr, V and Co in addition to Mo. This substitution is done to lower the cost of steel .Even though Mo tool steels are cheaper but are difficult to heat treat because of more tendency of oxidation, decarburization and grain growth as compared to W type High speed steels .This type is designated by M series.

W, Mo, Cr and V are carbide formers and hence forms respective carbides .These alloy carbides increases red hardness, wear resistance and cutting ability at high temperatures. In this respect V is most powerful carbide former and increases the resistance to grain coarsening at high service temperatures.

These steels are used for drills, taps, reamers, milling cutters, saws, lathe tools, punches, drawing dies, and wood working tools.

1.1.3 Heat treatment of HSS:-

This steel contains high amount of carbon (~0.9%) and high amount of alloying elements. Therefore special heat treatment cycle is applied for Hardening and Tempering of these steels.

The Steel is heated to 1250-13000C for austenitizing. Heating is done in stages to avoid thermal shocks and to homogenize the temperature throughout the specimen section. Austenitizing is followed by quenching in oil and then multiple tempering.

Tempering is done to eliminate the high amount of retained austenite after hardening which are due to presence of high amount of alloying elements which lowers the Mf temperature to below room temperature and hence large amount to austenite (~30%) doesn’t get transformed to martensite.

1.1.4 Effect of Cryotreatment:-

The microstructure of High speed steels shows as much as 30% retained austenite after quenching in oil at room temperature. Retained austenite lowers the hardness and thus the wear resistance of tool steel and therefore it is necessary to reduce this retained austenite to lower values.

For this, the steel is cooled below -1800C i.e. below Mf temperature (Martensite finish temp.)   to transform retained austenite to Martensite. For this purpose liquid Nitrogen is used.

1.2. M35 (Molybdenum type high speed steel):

Table 1.1 Composition of M35 HSS

| Element | C | W | Mo | Cr | V | Co | Mn |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Element (Wt. %) | 0.90 | 6.03 | 5.28 | 3.95 | 1.72 | 4.73 | 0.24 |

1.2.1 Heat treatment history of M35:

Hardening of M35 tool steel was done in the sintering tubular furnace with controlled heating in steps of and 550˚C then 900˚C for half an hour in argon atmosphere and finally 1200oC for 2 minutes followed by quenching in oil stirred bath. After hardening, the triple tempering (TTT) was carried out at 4000C for 2 hrs for each tempering cycle followed by air cooling to room temperature. The microstructure after hardening and tempering shows the alloy carbides of sub-angular to round shape in the matrix of tempered martensite.

1.2.2 Cryogenic treatment

The post cryogenic treatment was given to heat treated specimen as described in section 2.2 The cryosoaking time was varied from 4 hours to 48 hours. After regular interval of cryosoaking time, the specimens were removed from Cryoprocessor and immediately transferred and stored in a highly insulated thermocol box till the specimens attain the room temperature.

1.2. Effect of Cryotreatment on microstructure and Properties of M35 HSS :

Cryotreatment of the samples at -1860C for various soaking times results in variation of the hardness and Wear resistance. This may be due to precipitation of various alloy carbides when the samples are brought to room temperature from the cryogenic soaking temperature. The increase in carbide density results in increase in Hardness and Wear resistance. The increase in Wear resistance may be also due to various type of carbides present. Therefore, Microstructural Characterization of these samples is necessary to understand the effect of cryotreatment.

1.3 Objectives and Scope:

The objective of this project is to do characterization of alloy carbides present in the M35 tool steels cryotreated for various soaking time, in order to understand the effect of cryotreatment on carbide density, type of carbides present and Wear properties.

Scope of this project lies in the Characterization of alloy carbides and matrix which has been done by Electron Probe Microanalysis for the following objectives.

- To analyze by EPMA elemental distribution of alloying elements

- To identify carbides and their chemical composition at all stages of cryotreatment.

- To estimate shape and size of carbides.

Chapter II

Experimental Procedure

2.1 Sample Preparation for EPMA:

Sample Configuration: cylindrical shape samples of diameter 10mm and height 15mm.The samples were cold mounted by using Epoxy resins. Special cylindrical metal rings were used to mount the samples. The samples were then polished for a mirror finished surface followed by a gentle soap wash and Ultrasonic cleaning to remove any residual hydrocarbons from the surface.

2.2 Characterization Techniques: EPMA

Sample to be analyzed:

M35 HTTT- designated as sample 1

M35 HTC16- designated as sample 2

M35 HTC40- designated as sample 3

M35 HTC48- designated as sample 4

2.2.1 Electron Probe Micro-Analysis (EPMA)

2.2.1.1. Introduction:

Some of the modern methods of Characterization enables chemical analysis of a small (microscopic) region of materials. A spot of a phase or particle can be seen and it’s analysis can be carried out, something not possible by conventional characterization techniques.

2.2.1.2 Principle:

In EPMA, a small electron probe interacts with the sample resulting in various interaction products such as Back scattered Electrons, Secondary Electrons, and most importantly the characteristics X-rays of the elements present in the sample. These characteristic X-rays can be utilized for finding out the composition of a particular area of the sample.

Measurement of the energy of X-rays enables us to find out which elements are present. If one measures how many X-rays are emitted of any type per second (intensity of X-rays) which gives concentration of elements.

2.2.1.3 EPMA Unit:

The EPMA unit broadly consists of;

i)   An Electron source

ii)  Electromagnetic lens system

iii) Spectrometers (Wavelength Dispersive/ Energy Dispersive system)

iv) Detectors (e.g., proportional counters)

2.2.1.3 Principle of Working of EPMA:

The basic operating principles of the are illustrated in fig.1. An electron optical column containing an electron gun, magnetic lens, a specimen chamber and various detectors are maintained at vacuum of atleast 10-5 mm Hg. A directly heated filament provides a source of electron for the electron gun. The filament is held at a negative potential, 5 to 30 kV relative to the gun anode, which is grounded. A grid placed between the filament and the anode is biased at a potential slightly less than that of the filament. Thus electrons are attracted from the filament to the anode focused by the field of the grid cap. The electron gun acts as a lens, forming an image of the filament which is then demagnified by two or more magnetic lenses to form the final probe. The probe size is in the range of 0.1 to 1μm with corresponding probe currents in the range of about 10-1000 nA. When the focused electron beam strike the sample a variety of signals are generated, including  backscattered electrons, secondary electrons and X-rays. Although the backscattered electron signal varies with atomic number but mainly it is the X-rays that provides a unique way of performing both quantitative and qualitative analysis which can be detected by either CDS or EDS systems.

Fig.1. Showing constructional details of an EPMA unit

2.2.1.4 Electron Gun (Source of Electrons):

The source of electrons is a Tungsten filament of a hairpin Shape. The filament is heated by passing current through it and electrons are emitted by thermionic emission. The electron beam is repelled by a negatively charged Wehnelt cylinder and it is accelerated through the positively charged anode plate. The electron beam can be accelerated to 0.2 to 50 kV.

The tungsten filament can give electron beam of about 50μm diameter. For better illumination LaB6 (lanthanum-Hexaboride) filaments can be used which gives beam of 10μm diameter and hence better resolution and longer lifespan of filament.

2.2.1.5 Electromagnetic lenses:

The electron beam can be focused by magnetic fields obtained by using electromagnetic coils. These devises are called as electromagnetic lenses. In analogy with a conventional glass lens in optics, the electromagnetic lens has a focal length, depth of focus and resolving power.

The coils are enclosed in an iron casing whose inner tube has a non-magnetic core with an air gap. There are also special pole pieces with pole shoes to help in reducing the focal length. The current passing through the coils can be controlled to focus the electron beam.

Beam size is directly proportional to probe current. Typically, at 10-5A beam current the beam size is 2μm and at 10-12A beam current the beam size is 0.005mm.The beam current of the order of 0.5 to 300nA is possible.

The defects of Spherical and Chromatic aberration are vey important factors and should be minimized.

2.2.1.6 Electron Detectors:

Types of counters/ detectors;

1. Proportional Counter (has good resolution)

2. Geiger-Muller Counter (routine control under conditions of low count rate)

3. Scintillation Counter (for elements of higher atomic numbers than 24)

4. Solid state Detectors.

Electron detectors are used to detect back scattered and secondary electrons. The grid near the sample is kept at -50 V to avoid SE’s from being collected. The grid is kept at low positive voltage (320V) to collect the secondary Electrons by using Scintillation counter coupled with photomultiplier. Generally 6-8 detectors with large collection angles are used to separate Chemical and Topographical contrast.

2.2.1.7 Vacuum System:

In EPMA, the Specimen chamber, Spectrometer and Electron column are kept in a vacuum to the level of 10-4Pa with the help of oil diffusion pump and Rotary pumps.

The Electron gun is kept at 10-6Pa with the help of Ion Pump. Air locks are provided to exchange the sample or filament in the gun without venting the entire system. Contamination of sample is kept at minimum level.

2.2.1.8 X-ray detector:

In EPMA generally X-ray spectral measurements are performed using crystal-diffraction spectrometers (CDSs). The small fraction of the X-rays exits the electron optical column and enters the spectrometer where they impinge on the analyzing crystal. As the incident angle θ is varied, a maximum in X-ray intensity occurs at the detector when Bragg’s law,

n=2d sin θ

The X-ray detector most commonly used on the CDS is the proportional counter.

2.2.1.9 Proportional Counter :

Fig.2. Proportional Counter

It mainly consists of a grounded metal cylinder with an electrically isolated thin metal wire running up the centre. The wire is connected to a high voltage supply (1-3 kV) through a large current-limiting resistor. X-ray from the analyzing crystal enters through a thin window mounted on the side or end of the metal tube. When an individual X-ray photon enters the tube it causes the ejection of a photoelectron from an inert-gas atom. The photoelectron then ionizes other gas atoms and all of the electrons produced are attracted to the centre of the central anode wire. These electrons are then accelerated by the high voltage and they in turn produce secondary ionization. The total charge is then converted to a voltage pulse by a charge sensitive pre amplifier and then further increased by the main amplifier. The signal from the main amplifier is passed to a single-channel analyzer and then counted. Quantitative analysis normally involves scanning one or more crystals through their θ range and displaying X-ray intensities as a function of angle on a strip-chart recorder.

2.2.1.10 Spectrometers:

Two techniques are used for analyzing the X-ray spectrum:

1) Wave length Dispersive Spectrometry (WDS)

2) Energy Dispersive Spectroscopy (EDS)

2.2.1.11 Wave length Dispersive Spectroscopy (WDS):

In WDS, the characteristic x-rays are identified by their wavelengths by diffracting them on a Single crystal of known‘d’ spacing and following Bragg’s Law nλ=2dsinθ. Wave length dispersive spectrometer consists of crystal, proportional counter and pulse height analyzer. Different components of the system are shown in following (Fig.1)

In a fully focusing spectrometer sample, crystal and detector all lie on the same focusing circle called as Rowland circle such that Bragg’s Law is satisfied in all cases. In WDS, lithium doped Silicon single crystal Si (Li) is used.

Diffracted X-rays are detected with the help of proportional counters. Most commonly gas filled counters are used to detect X-rays. Generally Argon mixed with 10% methane (commercial gas P-10) is used in flow counters.

2.2.1.12 Energy Dispersive Spectroscopy (EDS):

In EDS, solid state detectors are used to detect X-ray lines emitted from the sample. In EDS, the various elements are detected by calculating the energy of the characteristic X-rays.

2.2.1.13 Crystals used in EPMA:

| Crystal | Full name | Composition | 2d(nm) | Elements which can be detected |
| --- | --- | --- | --- | --- |
| LiF | Lithium fluoride | LiF | 0.4207 | K: 21 Sc-37 Rb L: 52 Te onwards |
| PET | Penta Erithrotol | C5H12O4 | 0.8742 | K: 14 Si – 25 Mn L: 38 Sr – 65 Tb M: 73 Ta onwards |
| TAP | Thallium acid pthalate | C8H5O4Tl | 2.576 | K: 9 F – 15 P L: 25 Mn – 41 Nb M: 57 Ta – 80 Hg |
| PC1 | Pseudo crystal 1 | W/Si multilayer | 6 | K: 6Li – 9F |
| PC2 | Pseudo crystal 2 | Ni/C multilayer | 10 | K: 5 B – 8 O |
| PC3 | Pseudo crystal 3 | Mo/B4C multilayer | 20 | L: 4 Be – 5 B |

2.2.1.14 Applications Of EPMA:

- Compositional Analysis at micro-level

- EPMA can be used to determine phase diagrams.

- Diffusion studies

- Study of Geological Phases.

- Study of Biological Samples.

Chapter III

Results and Discussion

3.1 Microstructure of as received M35 HTTT:

3.1.1 Optical and Back Scattered Electron Image:

The Optical and Back Scattered image fig.3.1& Fig.3.2 Of M35 HTTT shows the presence of alloy carbides in the matrix of tempered martensite.

Fig.3.1. Cryotreated M35HTTT at a magnification of 500X and BSE Image (right)

V rich carbide

Matrix

W rich carbide

Fig.3.2 BSE image showing presence of W and V rich carbides

3.1.2 Qualitative Analysis of Carbides:

The back scattered electron image (Fig.3.2) shows the presence of a small dark V rich carbides and some large white W rich carbides. These carbides are identified by the WDS spectra.

Fig.3.2 WDS spectra of with TAP crystal

Fig.3.3 WDS spectra with LiF crystal

Fig.3.4 WDS spectra with PET crystal

The WDS spectra obtained from the white carbides shown in Fig.3.2 identifies the carbide as W rich carbides interpreted from the sharp peaks observed in the spectra Fig.3.2, Fig.3.3 and Fig.3.4. The other elements such as Fe, V and Mo are also detected from the above three WDS spectra.

3.2 Distribution of Alloying Elements:

3.2.1 Distribution of Cr :

Fig. 3.5 and Fig.3.6 shows the distribution of Cr with the help of the X-ray images.

Fig.3.5 Cr Ka (WDS) characteristics x-ray image.

Fig.3.5 shows homogeneous distribution of Cr in the matrix therefore it depicts that the Cr may be in the solid solution in the matrix.

Fig.3.7 BSE image with atomic number contrast.

W rich region

Fig.3.8 W Ma (WDS) characteristics X-ray Image.

Fig. 3.9 V Ka (WDS) characteristics x-ray image.

Comparison of Fig.3.8 and Fig.3.9 with the back scattered image Fig.3.7 identifies the W rich and V rich regions. This confirms the presence of W and V carbides in the matrix.

3.3 X-ray line scan of carbide:

Fig.3.10  V Ka X-ray line Scan.

A line scan across the carbide yielded the following results.

Fig.3.11 Elemental Distribution of W across the carbide from W Ma.

Fig. 3.12 Elemental Distribution of V across the carbide from V Ka.

The presence of V rich carbide can be interpreted from Fig.3.12 which scans from 0 to 9μm. The constant V profile between 3.7um and 4.7um indicates the V rich carbide core in agreement with the distribution shown in Fig.3.10 (V rich region shown in red colour).

3.4 Effect of Cryogenic soaking time on W and V rich carbides:

.

Fig.3.13 x-ray Image from W Ma (M35HTTT)                 Fig.3.14 X-ray image from V Ka (M35 HTTT)

2.

Fig.3.15 X-ray Image from W Ma (M35 HTC16)         Fig.3.16 X-ray image from V Ka (M35 HTC16)

3.

Fig.3.16 X-ray Image from W Ma (M35 HTC40)     Fig.3.18 X-ray image from V Ka (M35 HTC40)

4.

Fig.3.19 X-ray image from W Ma (M35 HTC48)        Fig.3.20 X-ray image from V Ka (M35 HTC 48)

From Fig.3.13, 3.15, 3.17 and Fig.3.19, it can be observed that the W rich region  has initially increased for HTC16 and decreased in Fig.3.16.  Again, the carbide density has found to be increased for HTC48 observed from Fig.3.19. Similar bahaviour is observed for V rich regions.

Chapter IV

SUMMARY

The Cryotreated M35 Molybdenum type High speed tool steel shows variation in carbide density and their distribution with respect to the cryosoaking time. To understand this phenomenon, the Microstructural Characterization of carbides was performed with the help of EPMA technique. X-ray image scan for W and V was done in order to understand their distribution in the matrix and to detect the variation in their carbide density.

The EPMA has confirmed the presence of W and V rich carbides in the matrix for all the cryotreated samples. The Cr and Mo are found to be homogeneously distributed throughout the matrix. No new type of precipitation of carbide was observed. The carbide density for W and V has maxima for HTC16 and HTC48 and minima for HTC40.

REFERENCES